## Slide 1: COMPUTATIONAL IMPLEMENTATION AND VALIDATION OF THE CONSTITUTIVE MODELS FOR HEAT RESISTANT DEVICES
Jovana Stojić, Massimo Penasa
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.

## Slide 2: TABLE OF CONTENTS
02
04
01
03
Basic information about the project and myself
Introduction
Outcome of the analysis and their validation
Results
Illustration of the problem regarding the analysis for the heat resistant device
Motivation
Goals and intentions regarding the topic
Future steps

## Slide 3: RE-FRACTURE2
Reducing the ecological footprint of the steel production
Simulating the behavior of the refractories over the entire working temperature range
Characterisation of the material model and implementation in the routines for finite elements computations

## Slide 4: MOTIVATION
Why refractories?
possess high thermal strength at elevated temperatures  widely used in steel and iron production
Wide working temperature range  fractures, thermal shock
Demand for the new refractory parts higher emission of CO2
Varying material properties dependent on the temperature  complex behavior

## Slide 5: ABOUT THE MODEL
Nonlinear thermomechanical analysis of a heat resistant device including:
Nonlinear surface flux (temperature, coordinates and time dependent)
Temperature dependent material properties
Submerging (molten steel)
Chart: Temperature
| 195 | 597 | 898 | 1200
specific heat | 1149.7 | 1443.5 | 1568.6 | 1832.6
conductivity | 0.0018203 | 0.001537 | 0.0015257 | 0.001736
expansion *1e3 | 0.0019308 | 0.0019597 | 0.0020394 | 0.0021013 | 0.0022032 | 0.0022863 | 0.0023279 | 0.0024118 | 0.0026022 | 0.0028972 | 0.0030637

## Slide 6: INCOUNTERED PROBLEMS
Python programming
Custom subroutine for the heat flux
High level of dependency
01
02

## Slide 7: STEP BY STEP
Nonlinear thermal analysis (only varying parameters)
Nonlinear thermal + linear mechanical analysis
Translation of the subroutine
Adaption of the commands using Python
Nonlinear thermomechanical analysis
01
02
03
04
05

## Slide 8: RESULTS COMPARISON
original
our results

## Slide 9: RESULTS COMPARISON
original
our results

## Slide 10: RESULTS COMPARISON
original
our results

## Slide 11: PLASTICITY MODEL
Decomposition of the strain tensor
ε
Flow rule
Yield function
Complementarity conditions
Numerical method (Newton’s tangent)
p
F(σ, k) = 0
F(σ, k) < 0

## Slide 12: PLASTICITY MODEL – DOUBLE DRUCKER PRAGER
Yield function
Different characteristics in tension and compression
Double Drucker Prager cone, whose top is on the hydrostatical axis

## Slide 13: PLASTICITY MODEL – RESULTS
Stress and plastic strain distribution
Focus on the parts under tension developed because of the expansion of the outside of the tube
Compression
Tension

## Slide 14: CASE STUDY- INITIAL CRACK
Initiated crack
Nonlinear thermomechanical analysis using Mazar's damage model
Potential collapse indication

## Slide 15: DAMAGE MODEL - MAZARS
Plasticity does not modify the elastic response of the material
Quasi-brittle - instead of the formation of one or few large cracks, the fracture failure is preceded by an elevated number of microcracks  introducing internal variables
Stress beyond the elastic limit inelastic deformation
Damage initiation criterion (deformation where damage starts) and a damage evolution criterion
The stress will still continue to grow for increasing values of strain, even if at a decreasing rate
Once the material reaches its peak stress (at some moderate value of the damage variable), the stress will start to decrease and follow its softening curve
Further damage can occur only if the strain reaches the maximum strain value measured in the previous load history
Bringing the peak stress closer to the damage initiation value that could be followed by a first rapid degradation while preserving the required energy dissipation for subsequent degradation at higher deformation levels
E - the material matrix
D - damage internal variable
- elastic strain

## Slide 16: DAMAGE MODEL - RESULTS
Internal variable indicating damage

## Slide 17: FUTURE PLANS
Validation of the models using mathematical programming
Acquiring the most suitable model for the refractory materials, accounting for different kind of nonlinearities
Extension of the FE software to allow the description of the thermoplastic instabilities
Fortran implementation of the constitutive model

## Slide 18
E-mail: stojic.jovana98@gmail.com
LinkedIn: Jovana Stojić
CAEmate
Sites: https://caemate.com
https://www.refracture2-h2020.eu
THANK YOU FOR YOUR ATTENTION!
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.