## Slide 1: Advanced ceramics and application conference X Serbian Ceramic Society
“Digital image correlation and inverse analysis for characterization of fracture properties”
Ilias Psilakis & Vladimir Buljak
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Sklodowska-Curie grant agreement No 955944 - RE-FRACTURE2.

## Slide 2
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
2
fm and gm are the mean grayscale values!
CLS  0 – Better match

## Slide 3
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
3
DIC is a valuable tool on planar surfaces where a suitable pattern is present or can be applied.

## Slide 4: Inverse Analysis Procedure
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
4
Parameters identification (experiment selection)
Numerical model (FEM simulation)
Sensitivity analysis (measurable quantities – variation of parameters)
Objective function  Minimization

## Slide 5: Compact Tension Specimen
Digital Image Correlation | Inverse Analysis | Case Study | Results | Next Steps | Conclusion
5

## Slide 6
Digital Image Correlation | Inverse Analysis | Case Study | Results | Next Steps | Conclusion
6

## Slide 7: The numerical model
Digital Image Correlation | Inverse Analysis | Case Study | Results | Next Steps | Conclusion
7
Zero thickness cohesive elements
(stress distribution)
Region Of Interest!
Elasticity Model
Damage Criterion

## Slide 8
Digital Image Correlation | Inverse Analysis | Case Study | Results | Next Steps | Conclusion
8
ω =f |Uexp – Ucom(x)|=f |r|
Nonlinear Least Squares (NLS)
Discrepancy Function (i.e. objective function)
Objective Function
Optimization Algorithm
1) Young Modulus 2) Damage Initiation
Parameters

## Slide 9
9
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion

## Slide 10
10
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion

## Slide 11
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
11

## Slide 12
12
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
To build more complex models
More parameters

## Slide 13
13
Digital Image Correlation | Inverse Analysis | Case study | Results | Next Steps | Conclusion
DIC
IA
GENERATING RESULTS – HANDLING DATA WITH MISSING INFORMATION

## Slide 14: Advanced ceramics and application conference X Serbian Ceramic Society
Thank you for your attention!
Ilias Psilakis
ipsilakis@mas.bg.ac.rs
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Sklodowska-Curie grant agreement No 955944 - RE-FRACTURE2.