## Slide 1: COMPUTATIONAL IMPLEMENTATION AND VALIDATION OF THE CONSTITUTIVE MODEL FOR THE REFRACTORY MATERIAL
Jovana Stojić, Massimo Penasa
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under the Marie Skłodowska-Curie grant agreement No 955944 – RE-FRACTURE2.​​

## Slide 2
4
1
2
3
TABLE OF CONTENTS
FUTURE STEPS
Goals and intentions regarding improvement
INTRODUCTION
Basic information about the personal role in the project RE-FRACTURE2
MOTIVATION
Illustration of the problem of defining and implementing the constitutive model for refractories
CURRENT STATE
Outcome of the analyses using developed subroutine and their validation

## Slide 3: INTRODUCTION
Implementation of the constitutive models for the high temperature behavior of refractory materials in routines for finite elements computations
Extension of the open-source FE software to allow the description of the thermoplastic instabilities
Applying the most advanced techniques for efficient solution of highly nonlinear problems
Chart: 
| CAEmate, Bolzano, Italy - 18 months | University of Belgrade, Serbia - 17 months | VESUVIUS, Ghlin, Belgium - 1 month
Hosting and secondmendt institutes | 18 | 17 | 1

## Slide 4: MOTIVATION
Possess high thermal strength at elevated temperatures  widely used in steel and iron production​
Wide working temperature range  fractures, thermal shock​
Demand for the new refractory parts  higher emission of CO2​
Varying material properties dependent on the temperature  complex behavior​
Critical component – ladle shroud; it is necessary for it to withstand thermal shock and high temperature range

## Slide 5: STAGES OF DEVELOPMENT
1
2
4
3
Cam Clay yield function; linear hardening
Cam Clay yield function; hardening with Bezier curves definition
Bigoni-Piccolroaz yield function; hardening with Bezier curves definition
Temperature dependency; customized function for elastic modulus

## Slide 6: BEZIER CURVES
3 points defined (pc, temperature, slope)
2 additional points obtained
2 second order curves
pc corresponding to the temperature retrieved

## Slide 7: VALIDATION OF THE YIELD POINT
finding the solution of the system of the equations
checking in the simulation results if the plastic deformation occurs; comparing the obtained third invariant and the pressure

## Slide 8
Results in Mathematica notebook for p and q
ABAQUS results for p and q using the developed UMAT

## Slide 9: DEFINITION OF THE HARDENING LAW
-

## Slide 10: BEHAVIOR IN COMPRESSION/TENSION
The curve obtained when specimen was loaded in compression
The curve obtained when specimen was loaded in tension

## Slide 11: COMPARING THE STATE VARIABLE PC
The curve obtained in the Python function
The curve extracted from ABAQUS results

## Slide 12: CANTILIEVER BEAM
Model of a beam in an uniaxial test (tension applied)
Different material properties' values, so the hardening law is nonlinear

## Slide 13: NONLINEAR HARDENING FOR THE BEAM MODEL
[-]

## Slide 14: SPHERICAL MODEL
Quarter of the sphere; internal surface blocked, on the external one the pressure is applied
Cumulative plastic strain as state variable number 14

## Slide 15: COMPONENT OF THE HEAT RESISTANT DEVICE (LADLE SHROUD)
Heat-resistant device loaded with pressure on the external surface

## Slide 16: FUTURE DEVELOPMENT
Redefinition of the hardening law
Linear/polynomial regression
Fitting the curve between the experimental points
Damage described using the phase field modeling

## Slide 17: THANK YOU FOR YOUR ATTENTION!
E-mail: stojic.jovana98@gmail.com
LinkedIn: Jovana Stojić
CAEmate
Sites: https://caemate.com
https://www.refracture2-h2020.eu